-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep3sp5fl.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

One Component, Snap Cure Epoxy Features High Strength Properties

Suitable for a variety of applications in the electronic, aerospace and OEM industries, Master Bond EP3SP5FL is a single component epoxy that cures in 1-2 minutes at 300°F. Since it requires heat curing, it essentially has “unlimited” working life at room temperature.

With a flowable, moderate viscosity, EP3SP5FL adheres well to a variety of substrates including metals, composites, glass, ceramics, many rubbers and plastics. It has a high tensile lap shear strength exceeding 2,000 psi at room temperature when bonding aluminum to aluminum. EP3SP5FL is an effective electrical insulator and it withstands thermal cycling, impact and shock. It also resists water, oils, fuels and has low shrinkage upon curing.

The service temperature range for this system is -60°F to +200°F. At ambient temperatures, EP3SP5FL has a hardness greater than 85 Shore D, but it softens above 200°F to 25-30 Shore D. This characteristic can allow the epoxy to be more readily reworkable than most other epoxy systems.

EP3SP5FL is available in syringes, ½ pints, pints and quarts containers. It has a minimum shelf life of 3 months and a maximum of 6 months in its original, unopened containers.

Master Bond High Bond Strength Epoxies

Master Bond EP3SP5FL is a moderate viscosity, snap cure epoxy that features the ability to be reworked. This one part system also features high physical strength properties. Read more about Master Bond’s epoxies with high tensile lap shear strength at http://www.masterbond.com/properties/high-shear-strength-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep3sp5fl

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #