-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/supreme-17ht

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Toughened, Low Outgassing, One Component Epoxy Features Thermal Cycling Resistance

Master Bond Supreme 17HT is a single component, no mix epoxy system for bonding and sealing applications featuring an unlimited working life at room temperature. “This thermally stable formulation has a high glass transition temperature of 410°F (210°C) and retains its bond strength at elevated temperatures,” says Rohit Ramnath, senior product engineer. “As a toughened system, it is ideal for bonding dissimilar substrates. Supreme 17HT’s unique combination of properties makes it suitable for applications involving repeated exposure to thermal cycling.” It also meets NASA low outgassing specifications per ASTM E595 testing.

Supreme 17HT possesses high bond strength properties with lap shear strength of 1,900-2,100 psi and tensile strength of 7,000-8,000 psi. This system is a reliable electrical insulator with volume resistivity of over 1015 ohm-cm at ambient temperatures and over 1012 ohm-cm at 400°F. It is serviceable from -100°F to +550°F (-73°C to 288°C). Along with its simple handling properties, Supreme 17HT offers a moderate viscosity of 100,000-150,000 cps.

Supreme 17HT cures at elevated temperatures with cure schedule options including 300°F for 5-6 hours or 350°F for 4-5 hours. It is available in standard packaging ranging from ½ pint to 5 gallon containers as well as specialty packaging including cartridges and syringes.

Master Bond Toughened Epoxy Systems

Supreme 17HT is a high strength, toughened epoxy adhesive ideal for applications that require resistance to high temperatures as well as thermal cycling. Read more about Master Bond’s flexibilized and toughened adhesive systems at https://www.masterbond.com/properties/flexibilized-and-toughened-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: httsp://www.masterbond.com/tds/supreme-17ht

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #